Ship-2-Shore (s-2-s) "Industrial & PLID” page 1 of 2

Applicators Guide for Inner Hulls - Ships, Barges, Tugs

S-2-S if applied indiscriminately causes a messy surface and is not appreciated by Lloyds, T.C., CSI's and others.

We are endeavouring to obtain these organizations approval, your co-operation is appreciated.

S-2-S is a high quality, high performance rust inhibitor, it is imperative it be applied

using a great deal of applicator discretion so as not to make a mess.

Spray gun settings: use a 12 to 15 thou. spray tip

Turn the pressure down until the product sprays gently, this reduces misting in the air.

On **Barge floors** only the cracks, seams, crevices and the flat part of the floor should

be coated, the top of the floor joists do not usually have a severe rust problem and this

is where people walk when inside so, don't apply product here unless there is a definite reason, unusual circumstances or a cat walk or plank walks are to be installed.

**Barge walls & Deck Heads:**  It is good practice to apply s-2-s **PLID** (thin) into the seam between the outer skin and the longitudinal, deck head, deck reinforcements and other crevices, (PLID will penetrate deeply into these areas protecting the structural integrity), top coat these areas and all other flat metal with **Industrial** (thick) using discretion if it maybe walked on.

**Voids -** Inspectors may need to crawl through these areas so where they must crawl or go in if the existing coating is mostly in fair condition but the lower section is rusty then apply a heavy (4 mils or so) coat of **Industrial** to the lower section as needed.

If deemed necessary apply a light coat over the existing coating or only apply coatings.

to areas that have problems usually the cracks, seams, welds etc. leaving a clean, uncoated path for inspectors to walk.

**Note:**

**When coating extremely old porous metal double up on the coating thickness - s-2-s has a tendency to penetrate right into the pores of the metal leaving nothing on the surface.**

 Ship-2-Shore (s-2-s) "Industrial & PLID” Dec 04 - Page 2 of 2

Applicators Guide for Inner Hulls - Ships, Barges, Tugs

**Ballast Tanks:**

Remove flaky rust scale (needle gun is fine)

Apply Ship-2-Shore Industrial.

Apply an extra heavy coat in the bottom foot or so of the tank.

Here water sloshes around, this lower area may need coating every few years

but there should be no preparation required.

Very easy maintenance.

**Optional:** Apply Ship-2-Shore PLID to all cracks, seams and crevices to penetrate in

 then coat everything with Ship-2-Shore Industrial.

**Caution**: Provide ventilation and wear an approved organic mist respirator when

 spraying in enclosed spaces.

 Refer to MSDS sheet.

The information contained here in is thought to be correct, the writer assumes no liability for errors, omissions etc.

MAXON TECHNOLOGIES

5400 WEST ROSECRANS AVE.

HAWTHORNE, CA 90250

PHONE: 424 - 236 - 4660

MAXONTECHNOLOGIES.COM